Bioinspired Graphene-based Nanocomposites Through Synergistic Effect

Qunfeng Cheng1*, and Lei Jiang1,2

1School of Chemistry and Environment, Beihang University, Beijing 100191, China
2Laboratory of Bioinspired Smart Interfacial Science, Technical Institute of Physics and Chemistry, Chinese Academy of Sciences, Beijing 100190, China
*Corresponding author email: cheng@buaa.edu.cn

Abstract: Graphene with extraordinary properties, strongest and stiffest material ever measured and the best-known electrical conductor, could have promising applications in many fields. However, processing graphene into high performance nanocomposites is very difficult. So far, graphene-based nanocomposites exhibit rather poor properties. It is a great challenge to assemble these micro-scale nanosheets into macro-sized nanocomposites for practical applications, for example, in aerospace, as flexible supercapacitor electrodes, artificial muscle, and tissue engineering. Where might one seek inspiration for making something new and original?

Nacre, the gold standard for biomimicry, provides an excellent example and guidelines for assembling two-dimensional nanosheets into high performance nanocomposites. The inspiration from nacre overcomes the bottleneck of traditional approaches for constructing nanocomposites, such as poor dispersion, low loading, and weak interface interactions. Graphene-based nanocomposites have been such a “hot topic” of late. Herein, we will focus on how to construct high-performance integrated graphene-based bioinspired nanocomposites through synergistic effect from interface interactions and building blocks based on our recent works.[1-3] Meanwhile we will also focus on a perspective of the dynamic area of bioinspired graphene-based nanocomposites, commenting on whether the concept is viable and practical, on what has been achieved to date, and most importantly what is likely to be achieved in the future.

Acknowledgements:

This work was financially supported by National Natural Science Foundation of China (21273017, 51103004).

References:

1. S. Wan, Y. Li, J. Peng, H. Hu, Q. Cheng, L. Jiang, ACS Nano 2015, 9, 708-714.

2. Q. Cheng, J. Duan, Q. Zhang, L. Jiang, ACS Nano 2015, 9, 2231-2234.

3. W. Cui, M. Li, J. Liu, B. Wang, C. Zhang, L. Jiang, Q. Cheng, ACS Nano 2014, 8, 9511-9517.

Author Biography

Qunfeng Cheng received his B.Sc. degree at Henan University (2003), and obtained Ph.D. degree at Zhejiang University (2003-2008). From 2008 to 2009, he worked in Tsinghua University and Florida State University as a Postdoctoral Research Fellow. In 2010, he joined BeiHang University. He is currently an Associate Professor at School of Chemistry and Environment, BeiHang University. His research interest focuses on high performance bioinspired polymer nanocomposites.

Note: The total length of the abstract should be no more than one page.